Theoretical study of a cobalt nano-contact
László Balogh1 *, Krisztián Palotás1, Bence Lazarovits2, László Udvardi1, László Szunyogh1
1 Department of Theoretical Physics, Budapest University of Technology and Economics
2 Research Institute for Solid State Physics and Optics, Hungarian Academy of Sciences
* E-mail: balogh@phy.bme.hu
Abstract
The recent technological development made it possible to build nano-sized structures which can play important role in wide range of applications. The theoretical studies exploring the quantum-effects of atomic-sized systems are of primary importance. In the present poster we investigate theoretically different properties of magnetic nano-particles.
   In order to model a break-junction a double pyramid cobalt nano-particle with a single cobalt atom between the tips of the pyramids has been chosen. The system was supported by two semi-infinite magnetically oppositely aligned Co substrate forming a domain wall through the contact.
   To find the magnetic ground state configuration two methods have been used and compared: simple magnetic model (continuous, isotropic Heisenberg model) and a density functional theory based electronic structure calculation.
   The magnetic configuration of the systems have been determined for various spatial separations of the substrates. We have found that the Neel type of domain wall is energetically more preferable then the Bloch wall for any length of the contact. The magnetic anisotropy energy of the central atom has been also analyzed. The anisotropy constants up to second order have been determined.
The physical system
Domain wall through the nano-contact
Naturally, a domain wall is formed through the nano-contact. The width of the domain-wall can be determined by fitting a hyperbolic tangent function. For the clear inter-pretation the width of the walls is normalized to the width of the domain wall belonging to x = 1. The slope of the curve is almost the same as the slope of the identity demonstrating that the width of the domain wall follows the change of the lengths of the point contact. The results of our calculations confirm Bruno's conclusion in Ref. 3.
Bloch
Global spin rotation around the [100] axis
We investigated the anisotropy effects, which are originated from the spin–orbit coupling, by plotting the band energy of the system under a rotation around the [100] axis. We expected an Eb = a1 cos(2) dependence on the polar angle coming from the uniaxial magnetic anisotropy. This investigation revealed that higher order components was also present in the anisotropy energy of the nano-contact.
Néel
The geometry of the contact viewed from the [100] direction. On the left, we depict the supporters below and above the double pyramids as blue rectangles. The cobalt atoms forming the cobalt contact are represented by brown balls. a denotes the nearest neighbor distance between the atoms in the fcc structure. We tuned the length of the contact via x, picking up the values 0.85, 0.90, 0.95, 1.00, 1.05, 1.10 and 1.15 in this study. (Note: only the marked distances were changed, all the others were unchanged.)
   On the right we present the embedded cluster. It consists of atoms from the supporters (blue balls), the cobalt nanocontact itself (brown balls) and the nearest neighbor shell around the contact (green balls). We indicate that the supporters are magnetized oppositely: [100] and [100] direction. (blue arrows)
Energy map of the central atom
Another investigation have been done in order to present the relevance of higher order terms beyound the simple Heisenberg model. All other spin directions were kept frozen into the ground state, while spin of the central atom was pointed into all directions. An energy map of the central atom was obtained and extraced in terms of the real spherical harmonics.
Isotropic Heisenberg model
Invariant under global spin rotation. The boun-dary conditions are invariants under global spin rotation around the [100] axis.
Configurations rotated around the [100] axis are equivalent.
Embedded cluster Korringa–Kohn–Rostoker method
The electronic structure of the contact has been determined by means of the embedded cluster Green's function technique as combined with the KKR method.1
   The higher order contributions can not be explained by only on-site anisotropy and pairwise exchange interactions.
References
1 B. Lazarovits, L. Szunyogh, and P. Weinberger, Phys. Rev. B 65, 104441 (2002).
2 A. I. Liechtenstein, et al., J. Mag. Mag. Materials 67, 65 (1987).
3 P. Bruno, Phys. Rev. Lett. 83, 2425 (1999).
Acknowledgements
Financial support was provided by the Hungarian Research Foundation (Contracts No. OTKA K77771) and by the New Hungary Development Plan (Project No. TÁMOP-4.2.1/B-09/1/KMR-2010-0002).
   The essential quantity of the EC-KKR method, namely the scattering path operator (SPO), corresponding to a finite cluster C embedded into a host system can be obtained from the above equation, Eq. (1), where th() and h() denote the single–site scattering matrix and the SPO matrix for the host confined to the sites in C, respectively, while tC denotes the single–site scattering matrices of the embedded atoms.
   A newly developped Newton–Raphson iteration is based on the gradients of the band energy (see Eq. (2)) against the transverse change of the exchange field, where F is the Fermi level and n() is the density of states.